| 品牌： | ROOKO瑞柯 | 税 率 |
| --- | --- | --- |
| 请选择对应 销售公司 | 宁波瑞品仪器有限公司 | 开具13%增值税专用发票 |
|  | 宁波盘羊仪器有限公司 | 开具3%增值税普通发票 |
| 开票品名/规格： | FT-401干粉灭火剂电绝缘性测试仪 |

FT-401干粉灭火剂电绝缘性测试仪

FT-401 Dry powder extinguishing agent electrical insulation tester

一、参照标准Basis：

参照标准GB4066.1-2004干粉灭火剂通用技术条件之电绝缘性要求而设计制造。用于检测干粉灭火剂之电绝缘性

design manufacturing according to National standard GB4066.1-2004 dry powder extinguishing agent general technical   conditions for electrical insulation requirements.To test the electrical insulation of powder extinguishing agent.

二、仪器组成部分Components：本仪器由耐压试验台部分、试验杯、电极、跌落试验台组成。

this instrument is consists of withstand voltage test platform , test cup, electrode and the drop test  platform.

三、技术参数：Technical parameters

1.试验杯：试验杯有一对安装在同一轴线上的圆盘形平板电极，杯体由不吸湿的高绝缘性材料制成。 圆盘形电极其他部位与试验杯的距离不小于13mm。试验杯的顶部与圆盘形电极顶部距离不小于32mm。试验杯可拆卸、清理和磨光，两个圆盘形电极间距离可调节。

1.Test cup: the test cup is provided with a pair of disc plate electrode arranged on the same axis. The cup body is made of non hygroscopic high insulation material. The distance between any part of the disc electrode and the test cup is not less than 13mm. The distance between the top of the test cup and the top of the disc electrode is not less than 32mm. The test cup can be disassembled, cleaned and polished, and the distance between the two disc electrodes can be adjusted.

2.圆盘形平板电极由抛光的黄铜板制成，直径为25mm，厚度不小于3mm，边缘成直角：两电极板间距为2.50±0.01mm

The disc plate electrode is made of polished brass, diameter is 25mm, thickness is not less than 3mm, edge forming right angle,

two electrodes spacing is 2.50±0.01mm.

3.耐电压试验部分，电压0-10Kv；电流输出0-20mA；数字显示

Withstand voltage test, voltage 0-10Kv, current output 0-20mA,

digital display.

4.跌落试验台:跌落高度30mm；允许负荷50kg 频率范围 0-1.667Hz连续可调，下落加速度大于9.3m／s^2。跌落次数500次使干粉灭火剂试样震实。

Drop test bench: maximum drop height 30mm, maximum allowable load 50kg, frequency range 0-1.667Hz continuously adjustable, falling acceleration is greater than9.3m／s^2.

Drop 500 times to jolt compaction of the dry powder fire extinguishing agent sample.

粉体综合分析解决方案：

FT-3400粉体流动行为分析仪（静态力学，剪切法）

FT-7100粉体流动测试仪（动态力学，转鼓法或旋转圆筒法）

FT-3900粉末屈服强度分析仪（单轴压缩法）

FT-3500粉体压缩强度测试仪（可压性，压缩方程）

FT-2000颗粒和粉末特性分析仪系列(传统方法)

FT-301系列粉末电阻率测试系统（电性能）

ROOKO瑞柯仪器

-------专注于粉体&新材料测量与分析仪器解决方案

----解决粉体表征：

流与不流分析  ；粒度；水分；体积分析；电导性、静电电荷分析.

----我们一直在做：

研发、生产、销售、租赁、实验室样品分析及后延扩展服务.